## Slide 1
과산화수소수 함유 관리용액의 사용법 미준수가
써클 소프트콘택트렌즈의 파라미터에 미치는 영향
황소담 ∙ 김채윤 ∙ 김승수 ∙ 박미정 ∙ 김소라
서울과학기술대학교 안경광학과
2021 한국안광학회 동계학술대회
INTRODUCTION
미생물에 의한 감염을 막기 위해 콘택트렌즈 착용 전후에 관리용액을 올바르게 이용하는 것의 중요성이 강조되고 있으나 관리 방법 인식 부족에 대한 문제점은 지속적으로 보고되고 있다.[1-3] 여러 관리용액 중 과산화수소가 포함된 관리용액은 사용 시 주의가 필요하며 제조사의 권장횟수를 벗어난 써클 소프트콘택트렌즈의 잦은 세척은 착색에 의한 착용감 저하 및 자극감을 유발할 수 있다.[4]
이에 본 연구에서는 과산화수소수가 함유된 관리용액의 사용법 미준수로 인해 써클 소프트콘택트렌즈의 파라미터에 어떠한 변화가 나타나는 가를 알아보고자 하였다.
METHODS
콘택트렌즈 착용자를 대상으로 렌즈 관리용액 사용실태에 대한 설문조사를 진행하였다. 설문 결과에 기반하여 AOSept Plus의 사용주기를 주 1회로 하여, 재질이 다른 5종의 써클 소프트콘택트렌즈를 각 렌즈의 교체주기에 따라 반복노출시켰다. 노출 전과 후의 렌즈의 중심두께, 직경, 곡률반경 및 광투과율을 측정하여 알아보았다.
RESULTS
설문조사 결과, 관리용액의 제조사가 제시한 권장횟수 미준수에 대한 응답이 59.5%로 나타났다. AOSept 반복 노출 후 모든 써클 소프트콘택트렌즈에서 중심두께는 증가하고 전체직경 및 곡률반경은 감소하여 전체적으로 렌즈가 스팁해짐을 알 수 있었다. 함수율이 낮은 써클렌즈보다 함수율이 높은 써클렌즈가 AOSept 노출로 인하여 더 큰 영향을 받을 수 있으므로 고함수 재질의 써클렌즈 착용 시에는 AOSept 사용법 준수에 대한 각별한 주의가 필요하다.
CONCLUSIONS
제조사의 권장횟수보다 과도한 사용을 하는 실태를 확인했으며 AOSept의 과도한 노출로 인해 써클 소프트콘택트렌즈의 파라미터에 통계적으로 유의한 변화를 초래함을 확인하였다. 콘택트렌즈 착용자들이 관리 용품의 사용에 대한 가이드라인을 준수하지 않을 시 렌즈의 변형이 유발될 수 있으므로 제조사 가이드라인의 숙지 및 준수의 중요성에 대한 교육이 필요하다고 판단된다.
REFERENCES
[1] Choi HJ, Yum JH, Lee JH, et al. Clinical features and compliance in patients with cosmetic contact lens-related complications. J Korean Ophthalmol Opt Soc. 2014;55(10):1445-1451.
[2] Park SJ, Lee SM, Kim MK, et al. Cosmetic contact lens-related complications: 9 cases. J Korean Ophthalmic Opt Soc. 2009;50(6):927-935.
[3] Choi HD, Kim YJ, Choi SY, et al. The state of eyewash solution use and parameter changes in clear soft contact lenses from repeated solution use. J Korean Ophthalmic Opt Soc. 2018;23(2):97-110.
[4] Lutzi FG, Chou BR, Egan DJ. Tinted hydrogel lenses permanency of tint. Am J Optom Physiol Optics. 1985;62(5):329-333.
Chart: Center thickness (mm)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 0.061667 | 0.084333 | 0.074333 | 0.075667 | 0.089667
after exposure to AOSept | 0.069185 | 0.085926 | 0.077556 | 0.085333 | 0.090407
Chart: Total diameter(mm)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 13.9 | 13.9667 | 14.4 | 14.0667 | 14.0333
after exposure to AOSept | 13.6444 | 13.8852 | 14.263 | 14 | 13.9667
Chart: Base curve (mm)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 8.2333 | 8.6333 | 8.8 | 8.5833 | 8.4
after exposure to AOSept | 7.75 | 8.2944 | 8.3722 | 8.3759 | 8.2944
Fig. 1. Change in central thickness of circle contact lenses according to repetition exposure to AOSept
Fig. 2. Change in base curve of circle contact lenses according to repetition exposure to AOSept
Fig. 3. Change in total diameter of circle contact lenses according to repetition exposure to AOSept
Chart: Transmittance(%)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 19 | 96 | 12 | 97 | 91
after exposure to AOSept | 18.6667 | 94.3333 | 10 | 97.1111 | 94.6667
Chart: Transmittance(%)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 65 | 99 | 75.6667 | 99.3333 | 94
after exposure to AOSept | 64.8889 | 96.8889 | 71.6667 | 98.8889 | 97.7778
Chart: Transmittance(%)
| Contact lensⅠ | Contact lensⅡ | Contact lensⅢ | Contact lensⅣ | Contact lensⅤ
baseline | 96.6667 | 99 | 97.3333 | 99.6667 | 95.6667
after exposure to AOSept | 97.3333 | 97.3333 | 97.8889 | 99.1111 | 98
UV-B
UV-A
Vis
Fig. 4. Change in transmittance of circle contact lenses according to repetiton exposure to AOSept